Section – IX

QUALITY ASSURANCE DOCUMENT

Table of Clauses:

1.	Quality Assurance by the Fabricator and Galvanizing Plant	44

1.1	Fabrication	44

1.1.1	Raw Material	44

1.1.2	Material Preparation	44

1.1.3	Assembly	44

1.1.4	Welding	45

1.1.5	Assembly Test	45

1.2	Galvanizing	45

1.2.1	Pickling (Acid Treatment)	45

1.2.2	Pre-flux (Fluxing)	45

1.2.3	Temperature of Zinc Bath	45

1.2.4	Zinc Coating	46

1.2.5	Quality Assurance	46

Section – IX

Quality Asurance Document

# 1.	Quality Assurance by the Fabricator and Galvanizing Plant

Fabricators/Galvanizing Plant should provide the quality assurance on their part. For this, Fabricators/Galvanizing Plant should maintain the in-process inspection and make QC logging. In-process inspection and QC logging should include from raw material up to the final product including all production process. In-process inspection and QC logging should be at following stages:

- Raw material

- Material preparation

- Assembly

- Welding

- Galvanizing

The Fabricator and Galvanizing Plant have to assure the quality of their products. That shall be done as per below.  Failing to provide the quality assurance, the fabricated and galvanized steel parts shall be rejected, even if the final product looks to be acceptable. It is near to impossible to check the quality of works only by inspecting the final product.

## 1.1	Fabrication

### 1.1.1	Raw Material

Test certificate should be provided by the manufacturer/supplier. All steel sections (steel grade Fe 410) should comply with the following requirement.

Yield stress ³ 250 N/mm2

Tensile strength ³ 410 N/mm2

Elongation ³ 23%

In-process Inspection Form should include the information as in table below:

### 1.1.2	Material Preparation

| S.no. | Date | Time | Particular | Section Size |  | Uniformity of Shape | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Thickness | Width |  |  |

* Permissible tolerance = ± 2.5%

### 1.1.3	Assembly

| S.no. | Date | Time | Drawing No | Particular | Conformity with Drawing | Finishing | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- | --- | --- |

### 1.1.4	Welding

| S.no. | Date | Time | Drawing No | Particular | Welding quality | Distortion | Size | Post Welding preparation | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

### 1.1.5	Assembly Test

| S.no. | Date | Time | Drawing No | Particular | Assembly test | Remarks | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- | --- | --- |

## 1.2	Galvanizing

### 1.2.1	Pickling (Acid Treatment)

| S.no | Date | Time | Observed (Required: PH Value =1 to 3, Density = Max 1.2 |  |  |  |  |  | Remarks | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | PH Value (PH Meter reading) |  |  | Density (Hydrometer reading) |  |  |  |  |
|  |  |  | Tank 1 | Tank 2 | Tank 3 | Tank 1 | Tank 2 | Tank 3 |  |  |

### 1.2.2	Pre-flux (Fluxing)

| S.no | Date | Time | Observed (Required Density = 1.10 to 1.15) | Remarks | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- |
|  |  |  | Density (Hydrometer reading) |  |  |

### 1.2.3	Temperature of Zinc Bath

| S.no | Date | Time | Observed (Required = 450 to 470°C) | Remarks | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- |

### 1.2.4	Zinc Coating

| S.no | Date | Time | Observed (Required = = 80 mm) | Remarks | Signature of QC Manager |
| --- | --- | --- | --- | --- | --- |

### 1.2.5	Quality Assurance

The Supplier shall ensure that the quality of work are following the Quality Assurance Document. The quality assurance of the fabricated steel parts including raw materials all complete is the sole responsibility of the respective Supplier following the standard “Quality Assurance Document” and must meet the required standards and fulfil the technical specifications and design drawings and  quality requirements.

However, from Purchaser’s side supervision and quality control of fabrication of bridge steel parts shall be performed by the NGO nominated by the Purchaser following the standard and format as per the “Quality Control Manual for Trail Bridge Construction”.

Fabrication Package, which is applicable only for Community Bridges, the respective fabricator provides the ‘Work Completion Report’ (WCR). In response to the WCR submitted by the fabricator, final inspection of the completed bridge steel parts is to be done though the assigned NGO on behalf of DDC's Office as per “Quality Control Manual and ToR for Construction Supervision and Quality Control”. However, endorsement of acceptance certificate of the bridge steel parts shall be done by the DDC's Engineer.

The work performed by the NGO shall be checked by the Purchaser’s Engineer, make suggestions/recommendations where necessary to the satisfaction of the Purchaser. Final acceptance of the fabrication of the steel parts shall be issued by the Inspecting Engineer/ Overseer and endorsed by the DDC's Office.

Final acceptance of the funding agency may require for donor-funded program.