4.	Material Specifications

###### Table of Contents

4.1	General 	32

4.1.1	Standards 	32

4.1.2	International System of Units 	32

4.2	Cable Structures 	33

4.2.1	Steel Wire Ropes 	33

4.2.2	Cable Terminals 	34

4.2.3	Cable Connections 	36

4.3	Steel Structures 	37

4.3.1	Structural Steel 	37

4.3.2	Fasteners 	38

4.3.3	Reinforcement Steel 	38

4.3.4	Increase of Permissible Stresses 	39

4.3.5	Rust Prevention 	39

4.4	Civil Structures 	40

4.4.1	Concrete 	40

4.4.2	Masonry 	41

4.4.3	Gabion 	42

4.4.4	Timber

4.5	Unit Weight of Construction Material 	43

4.1	General

4.1.1	Standards

The material specifications and permissible stresses for construction materials used for standard trail bridges are based on the latest Indian Standards (IS) available. Where IS were not available, other standards, such as DIN (German) Standards, British Standards, or SIA (Swiss) Standards, were considered.

4.1.2	International System of Units

The International System of Units (SI Units) has been introduced in this revised version according to IS 10005 - 1985.

| Quantity | SI Unit | Multiples |
| --- | --- | --- |
| Angle1) | – deg (degree, 3600) – grade (or gon 4009) | degree, minutes, seconds decimals |
| Length | m (meter) | (cm), mm |
| Area | m2 | (cm2), mm2 |
| Volume | m3 |  |
| Mass | kg (kilogram) | t (tonne) |
| Force | N (Newton) | kN (kilo Newton) |
| Moment of Force | Nm | kNm |
| Note: 1) The angle mode for the design analysis has been chosen to the degree unit (3600). Whereas for the survey, and the inclination of anchorage rods, it depends on the instruments used. |  |  |

Table 4.1.1: Selection of Common SI Units

Conversion of mass into force:

Force is the effect of gravitation g=9.81ms2on mass, therefore,

Force = 1 kg · g = 1 kg · 9.81 ms2= 9.81 kg⋅ms29.81 N  10 N.

For practical use, I kg is considered to be equal to 10 N (1 tone = 10000 N = 10 kN).

4.2	Cable Structures

4.2.1	Steel Wire Ropes

## A)	Specifications

Steel wire ropes should comply with all the requirements for:

IS 1835 – 1977	Steel Wire for Ropes

IS 6594 – 1977	Technical Supply Conditions for Wire Ropes and Strands

IS 9282– 1979	Specification for Wire Ropes and Strands for Suspension  Bridges

IS 9182 – 1979	Specification for Lubrications for Wire Strands and Ropes

## B)	Rope Particulars

Nominal diameters: 26, 32, 36, 40 mm

–	Construction: 	7 x 19 (12/6/1)

–	Lay: 	RHO, Right Hand Ordinary lay

–	Core: 	WSC, Wire Strand Core

–	Tensile strength of wire:	1570 N/mm2

–	Preforming: 	Preformed

–	Coating: 	Galvanized  “A” Heavy

–	Impregnation: 	Non-drying and non-bituminous type

–	Elongation: 	Pre-stretched

Nominal diameter: 13 mm

–	Construction:	7x7(6/1)

–	Lay: 	RHO

–	Core: 	WSC, Wire Strand Core

–	Tensile strength of wire: 	1570 N/mm2

–	Preforming: 	None

–	Coating: 	Galvanized "A” Heavy

–	Impregnation: 	Non-drying and non-bituminous type

## C)	Compiled Data

| Nominal Diameter (mm) | Approximate mass (kg/m) | Approximate Load (kN/m) | Metallic Area (mm2) | Minimum Breaking Load (kN) | Permissible Load (kN) |
| --- | --- | --- | --- | --- | --- |
| 13 | 0.64 | 0.0064 | 73 | 103 | 34 |
| 26 | 2.51 | 0.0251 | 292 | 386 | 129 |
| 32 | 3.80 | 0.0380 | 442 | 585 | 195 |
| 36 | 4.81 | 0.0481 | 560 | 740 | 247 |
| 40 | 5.94 | 0.0594 | 691 | 914 | 305 |
| Mean Value of Modulus of Elastic E = 110'000 N/mm2 = 110 kN/mm2 |  |  |  |  |  |

Table 4.2.1: Compiled Data of Steel Wire Ropes and Modulus of Elasticity

(including Safety Factor s = 3.0 for all cables and cable ending terminals)

4.2.2	Cable Terminals

## A)	Terminals with Drums in Concrete

Cables may be anchored directly into the foundations with the help of bollards (drums made out of steel) and secured with cable clamps. The cables should be wound 3 times around the drum in order to reduce the tensile force to be secured. The minimum diameter of the drums should be 0.95 m.

The friction factor between the cable and steel is taken to be   = 0. 1.

B)	Terminals with Sockets

Sockets should be manufactured from steel conforming to IS 226-1975, specifications for Structural Steel (Standard Quality) with a tensile strength of u = 420 to 540 N/mm2, normalized after the completion of machining operations and hot-dip galvanized.

Socketing should be made with pure zinc according to IS 3937-1974 (Part 1), Recommendations for Socketing of Wire Ropes.

Sockets can be used as an alternative to thimbles and bulldog grips for all cable anchorages except for those having diameters of 13 mm.

At present socketing is not used in Nepal.

| Nom. Diameter of Rope (mm) | ds (mm) | l (mm) | L (mm) | D1 (mm) | D2 (mm) | r (mm) |
| --- | --- | --- | --- | --- | --- | --- |
| 26 | 30 | 24 | 105 | 63 | 82 | 6.0 |
| 32 | 37 | 30 | 130 | 78 | 102 | 7.5 |
| 36 | 42 | 34 | 148 | 88 | 115 | 8.5 |
| 40 | 46 | 37 | 162 | 97 | 127 | 9.0 |

Table 4.2.2: Dimensions for Sockets

C) 	Terminals with Thimble and Bulldog Grips

Bulldog grips should conform to IS 2361-1970, Specifications for Bulldog Grips. The bridges must be drop-forged and suitably scored to grip a round strand rope of right-hand lay having six strands. Bridges, U-bolts, and nuts should be hot-dip galvanized with minimum zinc coating of 40 µm.

| Nom Diameter of Rope (mm) | A (mm) | B (mm) | C (mm) | D (mm) | E (mm) | F (mm) | G (mm) | H (mm) | I (mm) | Approximate Weight (kg) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 | M 12 | 64 | 27 | 32 | 15 | 51 | 12 | 28 | 22 | 0.28 |
| 26 | M 20 | 118 | 51 | 57 | 31 | 91 | 20 | 46 | 36 | 1.10 |
| 32 | M 20 | 124 | 54 | 59 | 34 | 94 | 20 | 46 | 36 | 1.30 |
| 36 | M 22 | 142 | 63 | 67 | 41 | 107 | 22 | 51 | 40 | 1.85 |
| 40 | M 25 | 157 | 69 | 75 | 44 | 119 | 25 | 58 | 45 | 2.40 |

Table 4.2.3: Dimensions and Weights for Bulldog Grips.

Bulldog grips, when properly applied, afford a simple and effective mechanical means of securing the ends of wire ropes, but have to be inspected after some loadings.

Thimbles are of open type, conforming to IS 2315 - 1978, Specifications for Thimbles for Wire Ropes. They must be forged and hot-dip galvanized with minimum zinc coating of 40 µm.

| Nom. Diameter of Rope (mm) | A (mm) | C (mm) | D (mm) | F (mm) | G (mm) | K (mm) | r (mm) | R (mm) | Approximate Weight (kg) | P (mm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 13 (14) | 41 | 19 | 68 | 15 | 9 | 12 | 7.5 | 9.5 | 0.12 | 38 |
| 26 (29) | 82 | 39 | 135 | 31 | 17 | 23 | 15.0 | 19.5 | 0.75 | 79 |
| 32 (32) | 92 | 43 | 152 | 34 | 19 | 26 | 17.0 | 21.5 | 1.85 | 89 |
| 36 (38) | 110 | 52 | 185 | 41 | 23 | 32 | 20.5 | 26.0 | 2.75 | 107 |
| 40 (41) | 124 | 47 | 208 | 44 | 26 | 36 | 23.0 | 28.5 | 3.20 | 121 |

Table 4.2.4: Dimensions and Weights for Thimbles (Nominal size of thimbles in b rackets)

Thimbles are necessary to give lateral support to the strands of the cable at the bend, and the pin must support the thimble.

P A - 3mm

##### Method and Specifications for Applying Bulldog Grips to Wire Ropes

| Nominal Diameter of Rope (mm) | Required Number, n, of Bulldog Grips | Gap "G" (mm) | Overlapping Length "L" (mm) |
| --- | --- | --- | --- |
| 13 | 3 | 80 | 550 |
| 26 | 5 | 155 | 1250 |
| 32 | 6 | 190 | 1700 |
| 36 | 7 | 215 | 2100 |
| 40 | 8 | 240 | 2550 |

Table 4.2.5: Terminals: Number of Bulldog Grips, Gap, Overlapping Length

The bridge of the grip must be fitted on to the working part of the rope and the U-bolt on to the rope tail. The first grip must be fitted as close as possible to the thimble. Grips should be spaced at a distance of approximately six times the rope diameter. The cable end should be protected from fraying with binding wire and, if the cable is too long, it should be fixed to the working part of the cable.

4.2.3	Cable Connections

Cable connections may be required because of a change in design or during erection of the bridge. If possible, the connection should be made with the same cable diameter or with the cable diameter that is next in sequence.

A)	Cables of Different Diameters

Cable connections of different diameters (or equal) must be made with the correct cable terminals (refer to 4.2.2 C) and a double pin intersection.

## B)	Cables of Equal Diameter

| Nominal Diameter of Rope (mm) | Required Number, n, of Bulldog Grips | Gap "G (mm) | Overlapping Length "L" (mm) |
| --- | --- | --- | --- |
| 13 | 6 | 80 | 700 |
| 26 | 10 | 155 | 1700 |
| 32 | 12 | 190 | 2400 |
| 36 | 14 | 215 | 3100 |
| 40 | 16 | 240 | 3900 |

Table 4.2.6: Cable Connections: Number of Bulldog Grips, Gap, Overlapping Length

Connections of cables equal in diameter can be made (refer to 4.2.2 C) without thimbles but with twice the number of bulldog grips.

4.3	Steel Structures

4.3.1	Structural Steel

## A)	Specifications

Structural steel should comply with all the requirements for:

IS 226 -1975 	Structural Steel

IS 800 -1984	General Construction in Steel

The tower design is based on the Swiss Standard SIA 161 (1979) for Steel Structures.

## B )	Steel Grade

Standard quality FE 410

## C)	Compiled Data

| Stress Case | Plate thickness (mm) | t  20 | 20 < t0  40 | t > 40 |
| --- | --- | --- | --- | --- |
|  | Bars (mm) | ø  20 | ø > 20 |  |
| Permissible Tensile Stress: at = 0.6 fy (N/mm2) |  | 150 | 144 | 138 |
| Permissible Compressive Stress: ac in (N/mm2) for slenderness  = 0 50 100 150 200 250 |  | 150 132 80 45 28 18 | 144 127 79 45 28 18 | 138 123 78 45 27 18 |
| Permissible Bending Stress in Tension: bt = 0.66 fy (N/mm2) |  | 165 | 158 | 152 |
| Permissible Bending Stress in Compression: bc in (N/mm2) (bc  0.66 fy); Elastic Critical Stress in Bending: Fcb =  1000 N/mm2 500 300 200 100 20 |  | 165 150 131 110 89 55 13 | 158 145 127 107 88 55 13 | 152 139 123 104 86 54 13 |
| Permissible Average Shear Stress: av. = 0.4 fy (N/mm2) |  | 100 | 96 | 92 |
| Maximum Permissible Equivalent Stress: P = 0.75 fy (N/mm2) |  | 188 | 180 | 173 |
| Maximum Permissible Equivalent Stress: e = 0.9 fy (N/mm2) |  | 225 | 216 | 207 |
| Modulus of Elasticity: E = 200'000 N/mm2 Unit Weight:  = 7850 kg/m3 |  |  |  |  |

Table 4.3. 1: Permissible Stress in Structural Steel

D)	Cold-formed Steel

Cold-formed steel should comply with all the requirements for:

| IS | 811 -1987 | Cold-formed Light Gauge Structural Steel Sections |
| --- | --- | --- |
| IS | 808 -1989 | Dimensions for Hot-rolled Steel Beams, Columns, Channels, and Angle Sections |

4.3.2	Fasteners

#### A)	Specifications

Bolts, nuts, and washers should comply with all the requirements for:

| IS | 1363 - 1984 (Part 1) | Hexagonal Head Bolts and Nuts |
| --- | --- | --- |
| IS | 1367 - 1983 | Threaded Fasteners |

### B)	Grade

Grade C, property Class 4.6

## C)	Compiled Data

| # Stress Case | Permissible Stress (N/mm2) |
| --- | --- |
| Stress in Axial Tension on Net Area tf | 80 |
| Stress in Shear on Gross Area: vf | 80 |
| Stress in Bearing on Gross Area: pf | 250 |
| Combined Tensile and Shear Stress | τVf calτvt+σtf calσtf 1.4 |

Table 4.3.2: Maximum Permissible Stress in Bolts for Class 4.6

4.3.3	Reinforcement Steel

A) Specifications

Reinforcement steel should comply with all the requirements for:

| IS | 1786 - 1986 | High Strength Deformed Steel Bars for Concrete Reinforcement |
| --- | --- | --- |
| IS | 456 -1978 | Plain and Reinforced Concrete |

## B)	Steel Grade

Fe 415, High Yield Strength Deformed Bars

C)	Compiled Data

| Stress Case | Permissible Stress for Fe 415 (N/mm2) |
| --- | --- |
| Tension Stress in Steel: st | 230 |
| Compression Stress in Steel sc | 190 |
| Permissible Bond Stress for Anchorage in Cement Mortar I : 1 and concrete > 1: 2 : 4 sB | 0.6 |
| Modulus of Elasticity: E = 210'000 (N/mm2) Unit Weight:  = 7850 (kg/m3) |  |

Table 4.3.3: Permissible Stress in Steel Reinforcement

4.3.4	Increase of Permissible Stresses

For occasional loadings combined with dead, live, and wind loads, the permissible stresses can be increased as follows:

| Load | Material | # Increase of Stress |
| --- | --- | --- |
| Dead load, live load, wind load and temperature, or wind load and seismic load | Structural Steel Bolts and Tension Rods Reinforcement Steel | 33% 25% 33% |
| Erection (Secondary Effects) | Structural Steel Bolts and Tension Rods | 25% 25% |

Table 4.3.4: Increase of Permissible Stress

4.3.5	Rust Prevention

To prevent rusting in steel structures they should be hot-dip galvanized or painted (painting is optional only but not recommended), and should comply with all the requirements for:

| IS | 8629 - 1977 | Protection of Iron and Steel Structures from Atmospheric Corrosion |
| --- | --- | --- |
| IS | 2629 - 1966 | Recommended Practice for Hot-Dip Galvanizing of Iron and Steel |
| IS | 4759 - 1984 | Specifications for Hot-Dip Zinc Coatings on Structural Steel |

4.4	Civil Structures

4.4.1	Concrete

A)	Specifications

Concrete should comply with all the requirements for:

IS 456 - 1978 		Plain and Reinforced Concrete

IS 269 -1989 		Ordinary Portland Cement

IS 383 -1970  		Coarse and Fine Aggregates

B)	Concrete Grades

(Mixed by volume units; cement: sand: aggregates)

– Lean concrete	1: 4: 8 used as sub-concrete

– Concrete	1: 3: 6    (M10)

– Concrete	1: 3: 6 mixed with 40% boulders

– Concrete	1: 3: 6 mixed with 60% boulders, used as fill concrete

– Concrete	1: 2: 4    (M15)

– Concrete	1: 1½ :3 (M20)

Reinforced concrete should always be vibrated.

C)	Compiled Data

| Grade of Concrete |  | Permissible Stress (N/mm2) |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | 1: 3: 6 (M 10) | 1: 3: 6 + 40% boulders | 1: 2:4 (M 15) | 1: 1½ :3 (M 20) |
| Stress in Compression | bending c (extreme fiber) | 3.0 | 2.0 | 5.0 | 7.0 |
|  | direct a | 2.5 | 1.5 | 4.0 | 5.0 |
| Shear stress, measured as inclined tension c |  | 0.3 | 0.2 | 0.5 | 0.7 |
| Stress in bearing |  | 2.0 | 1.0 | 3.0 | 4.0 |
| Tension stress in bending (plain concrete) |  | 0.3 | 0.2 | 0.5 | 0.7 |

Table 4.4.1: Permissible Stresses for Concrete

For occasional loading (wind, erection) combined with dead and live loads, the permissible stresses can be increased by 33%.

Modulus of Elasticity for Concrete 1: 2: 4 (M 15) and 1: 1½ :3 (M 20): E = 21000 N/mm2

In anchorage steel designs, the bond resistance of connection flats and rods and the bearing resistance of shuttering have generally been neglected.

4.4.2	Masonry

A)	Specifications

The specifications and permissible stresses given below are based on:

IS 1597 – 1967 (Part 1)	Code of Practice for Construction of Stone Masonry

SIA 178 – 1980	Swiss Standard for Stone Masonry

IS 2250 – 1981	Preparation and Use of Masonry Mortars

B)	Types of Masonry

(mixed by volume units; cement: sand)

–	Rubble masonry 	1: 6

–	Rubble masonry	1:4

–	Block stone masonry 	1:4

C)	Compiled Data

| Type of Masonry |  | Permissible Stress (N/mm2) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Rubble masonry 1:6 |  | Rubble masonry 1:4 |  | Block stone masonry 1:4 |  |  |  |
|  |  |  |  |  |  | Stratified blocks |  | Non-stratified blocks |  |
| Slenderness Ratio h/d* |  | 0.5 | 2.0 | 0.5 | 2.0 | 0.5 | 2.0 | 0.5 | 2.0 |
| Stress in Compression | bending (extreme fiber) | 1.3 | 0.7 | 1.9 | 1.1 | 2.1 | 1.3 | 3.7 | 2.0 |
|  | direct | 1.0 | 0.5 | 1.4 | 0.8 | 1.6 | 1.0 | 2.8 | 1.5 |
| Tension stress in bending |  | 0.13 | 0.07 | 0.19 | 0.11 | 0.21 | 0.13 | 0.37 | 0.20 |
| * h = height of wall, d = thickness of wall |  |  |  |  |  |  |  |  |  |

Table 4.4.2: Permissible Stress for Masonry

If masonry walls are used in combination with concrete and the thickness of the concrete is greater than the thickness of the masonry, the permissible stresses for the appropriate concrete grade have to be applied.

4.4.3	Gabion

A)	Specifications of Wire

Gabion wire should comply with all the requirements for:

IS 280	–1978		Mild Steel Wire for General Engineering Purposes

IS 4826	– 1979		Hot-dipped Galvanized Coatings on Round Steel Wire

B)	Diameter of Wire

Mesh wire	10 SWG

Selvedge wire	7 SWG

Binding Wire	12 SWG

4.4.4	Timber

## A)	Specifications

Timber should comply with all the requirements for:

IS	883	-1970	Design for Structural Timber

IS	1141    - 1973	Seasoning of Timber

IS	401	-1967 	Preservation of Timber

B)	Types of Timber

–	For walkway deck:

Group B (Modulus of Elasticity above 9800 and up to 12600 N/mm2)

–	For formwork:

Group C (Modulus of Elasticity above 5600 and up to 9800 N/mm2)

The wood for decking should be property seasoned and preserved either with coal tar creosote, with a mixture of coal tar and kerosene, or with a chemical-type preservative. If creosote or tar/kerosene are used for protection, a deep impregnation of the preservative must be obtained; surface application has little value.

C)	Compiled Data

| Stress Case | Permissible Stress and Modulus of Elasticity (N/mm2) |  |
| --- | --- | --- |
|  | Group B | Group C |
| Stress in bending tension along grain (extreme fibre) fb | 130 | 70 |
| Shear stress along grain | 1.3 | 1.0 |
| Stress in compression parallel to grain fcp perpendicular to grain fcn | 9.0 3.5 | 5.0 1.5 |
| Modulus of Elasticity E | 12700 | 9400 |
| Unit Weight (kg/m3) | 900 | 600 |

Table 4.4.3: Average Permissible Stress, Modulus of Elasticity, and Unit Weight of Timber

4.5	Unit Weight of Construction Material

The unit weight (mass) of construction material used in standard bridge construction is given in the following table. (For the purpose of load calculation, the weight (mass) is converted into SI units with the approximate value of 1 kg =10 N = 0.01 kN.)

| Material | Weight (kg/m3) | Load (kN/m3) |
| --- | --- | --- |
| Concrete: | 2200 | 22.0 |
| Masonry: |  |  |
| – dry rubble | 2000 | 20.0 |
| – rubble | 2200 | 22.0 |
| Steel | 7850 | 78.5 |
| Gabion | 1600 | 16.00 |
| Water | 1000 | 10.0 |
| Soil (According to survey and geological report) | 1600 to 2200 | 16.0 to 22.0 |
| Timber for walkway deck (sal wood) | 900 | 9.0 |

Table 4.4.4: Unit Weight of Construction Material

New IS 9282 - 2000 has reduced the breaking load. Nevertheless, for trail bridges, the IS 9282 – 1979 shall be effective.

Pre-stretching should be done by cyclic loading of the rope to 5% to 40% of the minimum breaking load in sequence of 5% to 10%, 5% to 20% and 5% to 40% loading till elongation stabilizes.